## Slide 1: Assessment of neurotrophin-loaded cryogel microcarriers for improving engraftment of human iPSC-derived dopaminergic progenitors
Saoirse Ryan
PhD Candidate
Supervisors: Prof Eilís Dowd & Dr Declan McKernan

## Slide 2
Cellular-based brain repair
Cellular based brain repair is a therapeutic option to treat Parkinson’s disease
Engraftment remains limited with poor survival and differentiation of iPSCs in situ in the brain
(Jarrin et al., 2021)
(Comini and Dowd 2024)
Cells are taken from their neurotrophin enriched environment
Poor differentiation in various species
Median Survival ~51% but median differentiation ~3%

## Slide 3
Cryogel Microcarriers
Increase the retention of neurotrophins
Sustained release of neurotrophins
Help cell survival and reinnervation
(Hakami et al 2024)
(Narasimhan et al 2024)
Negatively charged cryogel microcarriers -> 3-sulfopropyl acrylate (SPA) and poly (ethylene glycol) diacrylate (PEGDA)
GDNF and BDNF could be loaded to the microcarriers and released in a controlled manner over weeks and months
Microcarriers can potentially aid with engraftment of iPSC-DAPs

## Slide 4
Survival of dopaminergic neurons
Cryogel Microcarriers
(Hakami et al 2024)
(Narasimhan et al 2024)
Cytocompatibility
Functionality
Biocompatibility
TH+ fibre sprouting
Rationale for using microcarriers -> They can deliver neurotrophins to the cells so that the cells aren’t deprived in the diseased environment

## Slide 5
Aims and Hypothesis
Hypothesis: Microcarriers are cytocompatible with iPSC-DAPs and therefore potentially could improve the survival and differentiation of iPSC-DAPs in situ in the brain
Aim
Improve engraftment of iPSC-derived dopaminergic progenitors (iPSC-DAPs)
Phase 1
Determine if microcarriers are cytocompatible with iPSC-DAPs

## Slide 6
Methodology
iPSCs = Induced Pluripotent Stem Cells, SPA = 3-sulfopropyl acrylate, PEGDA = Poly (ethylene glycol) diacrylate

## Slide 7
Results – Human Nuclei Staining – Cell Survival
Group x Time F(4,43) = 0.523, p>0.05
Group x Time F(4,43) = 1.427, p>0.05
Cells Alone
Cells & microcarriers
Cells & tagged microcarriers

## Slide 8
Results – STEM121 Staining – Cell Survival
Group x Time F(4,43) = 1.691, p>0.05
Group x Time F(4,43) = 1.162, p>0.05
Cells Alone
Cells & microcarriers
Cells & tagged microcarriers

## Slide 9
Results – OX42 Staining – Microgliosis
Cells Alone
Cells & microcarriers
Cells & tagged microcarriers
Group x Time F(4,43) = 0.5417, p>0.05
Group x Time F(4,43) = 1.330, p>0.05

## Slide 10
Results – GFAP Staining – Astrocytosis
Cells Alone
Cells & microcarriers
Cells & tagged microcarriers
Group x Time F(4,43) = 0.1842, p>0.05
Group x Time F(4,43) = 0.3293, p>0.05

## Slide 11
Results – Fluorescence
DAPI
TH
OTX2
FOXA2
Immunocytochemistry
Tagged Microcarriers
HuNu
DAPI
DAPI
Immunofluorescence

## Slide 12
Discussion and Conclusion
Further studies should focus on testing the neurotrophin-loaded microcarriers with RM3.5 iPSC-DAPs to evaluate their potential and investigate if the microcarriers can enhance cell survival and differentiation.
The microcarriers did not affect cell survival (Human Nuclei and Stem121 staining), microgliosis (OX42 staining) or astrocytosis (GFAP staining) when compared to cells alone. The microcarriers are cytocompatible and biocompatible.
The fluorescently tagged microcarriers remained successfully labelled in vivo and the RM3.5 iPSC-DAPs showed promising differentiation patterns in vitro.

## Slide 13
Acknowledgments
University of Galway
Prof Eilís Dowd
Dr Declan McKernan
Dr Giulia Comini
Ms Sarah Crudden
Mr Tommy Patton
Ms Sienna Stucke
Ms Robyn Gaffey
Cardiff University
Dr Ben Newland
Dr Abrar Hakami
Dr Sophie Hill
The University of Edinburgh
Prof Tilo Kunath
Dr Nicola Drummond
Ms Michela Barbato
The Florey Institute, The University of Melbourne
Prof Clare Parish
Dr Niamh Moriarty
Funding
Research Ireland - GOIPG/2023/3047

## Slide 14
References
Comini G, Dowd E. A systematic review of progenitor survival and maturation in Parkinsonian models. Neural Regen Res. 2024 Nov 13. doi: 10.4103/NRR.NRR-D-24-00894. Epub ahead of print. PMID: 39589166.
Comini, G., & Dowd, E. (2025). The loaded matrix: neurotrophin-enriched hydrogels for stem cell brain repair in Parkinson's disease. Neural regeneration research, 20(8), 2315–2316.
Hakami A, Narasimhan K, Comini G, Thiele J, Werner C, Dowd E, Newland B. Cryogel microcarriers for sustained local delivery of growth factors to the brain. J Control Release. 2024 May;369:404-419.
JARRIN, S., CABRÉ, S. & DOWD, E. 2021. The potential of biomaterials for central nervous system cellular repair. Neurochemistry International, 144, 104971.
Narasimhan, K., Hakami, A., Comini, G., Patton, T., Newland, B., & Dowd, E. (2024). Cryogel microcarriers loaded with glial cell line-derived neurotrophic factor enhance the engraftment of primary dopaminergic neurons in a rat model of Parkinson's disease. Journal of neural engineering, 21(5).